## Slide 1: Presentation Order: Used a Random Number Generator
If anyone would like to volunteer to go earlier, that is also fine
Gavin
Caleb Monday, November 28
Nate
Justin
Elizabeth
Parker Wednesday, November 30
Nick
Trenton
Sulaiman
James
Peter
Samantha
A speaker from NASA offered to come talk to us on Friday of this week. Are we ok with there being a break?
Week after Thanksgiving
One more lecture. Any requests? Examples:
More on semiconductors (defects, DOS, p-n junctions)
X-ray absorption spectroscopy (beamline work)

## Slide 2
(or Laser)

## Slide 3
(or Laser)

## Slide 4
(or Laser)
Rotating the target and/or substrate improves uniformity

## Slide 5: Both MBE and PLD use RHEED to optimize (Reflection High Energy Electron Diffraction)
Substrate
Target(s)
Laser (often 248 nm)
Electron Gun
Electron Detector
Laser
MBE
Pulsed Laser Deposition (PLD)

## Slide 6: Reflection High Energy Electron Diffraction (RHEED)
Notes: But the same could be said for making weapons before they were automated.

## Slide 7: Reflection High Energy Electron Diffraction (RHEED)
Sample growth with MBE or PLD is sometimes referred to as an art. Every chamber is different. Have to optimize!
Notes: But the same could be said for making weapons before they were automated.

## Slide 8: The RHEED Pattern
You actually get a full RHEED pattern, not just an intensity.
a) RHEED pattern of bare TiO2-terminated SrTiO3 substrate
b) pattern for a substrate exhibiting mixed terminations
c) LSMO film after deposition was completed.
Most people just monitor the main peak, but there may be value in monitoring other peaks that identify other structures.

## Slide 9: RHEED Oscillations (Main Peak)
One of the things you can control during growth is the oxygen background pressure. What are some things you notice as we change the pressure?
What does it mean for the intensity to go down?
Is the wavelength of the oscillations changing? Why?
Notes: Note that the wavelength increase as oxygen pressure increases. Why? (More oxygen in the way during growth. Slows down growth. Not necessarily a d bad thing.)
What does it mean for the intensity to go down? Surface is getting rougher. Sometimes it can get better too.

## Slide 10: Material Growth Modes
Some materials rather clump together.
Others form flat layers. Some in between.
~ depends on whether the atoms would rather bond to the substrate or itself
Notes: You can roughly think about it as depending on whether the atoms would rather bond to the substrate or itself. The real quantity to look into would be the surface energy, but that’s not something we are really going into in this class.

## Slide 11: How do you determine sample quality?
Here are some techniques:
Diffraction (secondary phases, symmetry, periodicity, etc.)
Electron microscopy
Atomic force microscopy (surface smoothness)
Notes: It’s a hard question actually. There are a few obvious ways, but there are other ways that depend on what you want to do with the sample. And what does quality mean? Depends on the purpose.

## Slide 12: No sample is perfect Defects reading in Kittel: 585-595

## Slide 13: Defects in Solids
Mechanical and electrical properties of solids depend strongly on amount of defects
How would you expect this crack to affect material properties?
Notes: Actually, these are not pictures of atoms, which is even more obvious if you look at the scale I cut off. These are polystyrene spheres for self-assembled photonic crystals with intentional low-dimensional defects for defect-mode pass-band in stop-band of photonic bandgap. But, they do help might my point. 
How would you expect the defects show to affect the properties of the material? The big crack would certainly affect material strength. Also, it would likely be hard to flow valence electrons across that crack.

## Slide 14: Defects in Solids
Mechanical and electrical properties of solids depend strongly on amount of defects
Surface/interface reconstruction sometimes treated as defect (topic of next class)
Notes: Actually, these are not pictures of atoms, which is even more obvious if you look at the scale I cut off. These are polystyrene spheres for self-assembled photonic crystals with intentional low-dimensional defects for defect-mode pass-band in stop-band of photonic bandgap. But, they do help make my point. 
How would you expect the defects show to affect the properties of the material? The big crack would certainly affect material strength. Also, it would likely be hard to flow valence electrons across that crack.

## Slide 15: Types of Defects
Vacancy
(atoms don’t always get closer, why?)
Ideal Crystal
Notes: Self interstitial cause such a distortion to the lattice, that they rarely form. (high energy)
When might a line defect be favorable? When growing a material on another.

## Slide 16: Types of Defects
Vacancy
(atoms don’t always get closer, why?)
Substitutional
Ideal Crystal
Impurities of different atoms
Notes: Self interstitial cause such a distortion to the lattice, that they rarely form. (high energy)
When might a line defect be favorable? When growing a material on another.

## Slide 17: Types of Defects
Vacancy
(atoms don’t always get closer, why?)
Interstitial
Substitutional
Ideal Crystal
  Interstitial just means between the atoms. You can have a self-interstitial defect too.
Impurities of different atoms
Notes: Self interstitial cause such a distortion to the lattice, that they rarely form. (high energy)
When might a line defect be favorable? When growing a material on another.

## Slide 18: Types of Defects
Vacancy
(atoms don’t always get closer, why?)
Interstitial
Substitutional
Ideal Crystal
  Interstitial just means between the atoms. You can have a self-interstitial defect too.
Impurities of different atoms
Self-interstitial + nearby vacancy called Frenkel defect
Notes: Self interstitial cause such a distortion to the lattice, that they rarely form. (high energy)
When might a line defect be favorable? When growing a material on another.

## Slide 19: Types of Defects
Vacancy
(atoms don’t always get closer, why?)
Interstitial
Substitutional
Ideal Crystal
  These are all point defects (aka Schottky defects)
  which consist of only one or a few atoms, does not necessarily involve foreign atoms
  Interstitial just means between the atoms. You can have a self-interstitial defect too.
Impurities of different atoms
Self-interstitial + nearby vacancy called Frenkel defect
Notes: Self interstitial cause such a distortion to the lattice, that they rarely form. (high energy)
When might a line defect be favorable? When growing a material on another.

## Slide 20: Modeling Vacancies
What information do you think might be important to model bonds?
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 21: Modeling Vacancies
  Vacancies modeled by considering the energy Ev required to break the bonds between an atom inside the crystal and its nearest neighbors
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 22: Modeling Vacancies
  Vacancies modeled by considering the energy Ev required to break the bonds between an atom inside the crystal and its nearest neighbors
  Discussion: Compare the expected number of vacancies in an ionic material to a metal.
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 23: Modeling Vacancies
  Vacancies modeled by considering the energy Ev required to break the bonds between an atom inside the crystal and its nearest neighbors
  Discussion: Compare the expected number of vacancies in an ionic material to a metal.
  Vacancies in ionic materials tend to come in pairs (neutrality)
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 24: Modeling Vacancies
  Vacancies modeled by considering the energy Ev required to break the bonds between an atom inside the crystal and its nearest neighbors
  Discussion: Compare the expected number of vacancies in an ionic material to a metal.
  Vacancies in ionic materials tend to come in pairs (neutrality)
  Number of vacancies n = N exp (-Ev/kBT) where N= number of lattice sites, kB is Boltzmann’s constant
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 25: Modeling Vacancies
  Vacancies modeled by considering the energy Ev required to break the bonds between an atom inside the crystal and its nearest neighbors
  Discussion: Compare the expected number of vacancies in an ionic material to a metal.
  Vacancies in ionic materials tend to come in pairs (neutrality)
  Number of vacancies n = N exp (-Ev/kBT) where N= number of lattice sites, kB is Boltzmann’s constant
  Frenkel changes factor of ½ and N to NN’, interstitial sites N’
Notes: Bonds are stronger in ionic and covalent materials so vacancy energy should be higher. Thus ionic should have less vacancies than metal.
Also, vacancies in ionic materials tend to come in pairs to keep material charge neutral. If not, will likely get other stuff coming into system to balance the charge.
Treat ionic defects similar to Frenkel defects.
Irradiating and deformation can cause a lot of Frenkel defects

## Slide 26: Where would you expect an interstitial to go in a lattice with a one atom basis?
FCC
YouTube videos to further explain:
https://www.youtube.com/watch?v=4AW9PFWaMcQ
https://www.youtube.com/watch?v=ZuWMA8JvgjM
Notes: Sc first, in center
Fcc next, also in center but edges also likely
Bcc, face center
Videos after discussing this:
Maybe cut first video before cell projection (not necessary, maybe confusing for some, but it does relate back to early crystal structure stuff)
I’m debating on whether I like the second video better, but it takes more time. Motivates a little more

## Slide 27: High Purity Aluminum
has a variety of applications
If you get a sheet of aluminum (1 ft x 1 ft by .5 inch), what will be the total number of aluminum atoms at 20C and approximate the number of vacancies expected at 160, 200, 300 and 900K if the energy to create a vacancy is 0.75 eV?
Notes: Melting point of aluminum if 933 K.
If you have a one atom basis, the number of lattice sites is the same as the number of atoms
Yes the volume of the material will increase as heated.

## Slide 28: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
is a line defect
Notes: Start at M and count a 3x4 box around

## Slide 29: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
is a line defect
Notes: Start at M and count a 3x4 box around

## Slide 30: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
is a line defect
3
Notes: Start at M and count a 3x4 box around

## Slide 31: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
is a line defect
3
4
Notes: Start at M and count a 3x4 box around

## Slide 32: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
is a line defect
3
3
4
Notes: Start at M and count a 3x4 box around

## Slide 33: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
is a line defect
3
3
4
4
Notes: Start at M and count a 3x4 box around

## Slide 34: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
  Edge dislocation: Burgers vector perpendicular to dislocation line
is a line defect
3
3
4
4
Notes: Start at M and count a 3x4 box around

## Slide 35: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
  Edge dislocation: Burgers vector perpendicular to dislocation line
  Screw dislocation: Burgers vector parallel to dislocation line
is a line defect
3
4
3
4
Notes: Start at M and count a 3x4 box around

## Slide 36: Dislocations
Two-dimensional defect
Dislocation is a common one
Results from local elastic stress
Described by Burgers vector
  Constructed via closed loop around dislocation core
  Edge dislocation: Burgers vector perpendicular to dislocation line
  Screw dislocation: Burgers vector parallel to dislocation line
  Real dislocations are often a mix
is a line defect
Screw dislocation
3
4
3
4
Notes: Start at M and count a 3x4 box around

## Slide 37: How would you make a stack of sandwiches look like a screw dislocation?

## Slide 38: How would you make a stack of sandwiches look like a screw dislocation?

## Slide 39: What kind of dislocation is this?
Notes: Corn = edge dislocation

## Slide 40: What kind of dislocation is this?
Notes: Corn = edge dislocation

## Slide 41: Planar Defects
One case is a twin boundary (plane)
  Essentially a reflection of atom positions across the twinning plane.
Stacking faults
  For FCC metals an error in ABCABC packing sequence
  Ex: ABCABABC
Adapted from Fig. 4.9, Callister 7e.

## Slide 42
Close packed crystals
A plane
B plane
C plane
A plane
…ABCABCABC… packing
[Face Centered Cubic (FCC)]
…ABABAB… packing
[Hexagonal Close Packing (HCP)]
Notes: 0.74 for both fcc and hcp

## Slide 43: Stacking Faults

## Slide 44
    Defects in Metallic Crystals
      Most metals crystallize in bcc, fcc or hcp structures
      Changing pressure or temp. can interchange these forms for a metal
      Soft and malleable metals usually have fcc structure (copper)
      Harder and more brittle metals usually have the hcp structure (zinc)
        Atoms can slide past each other and then realign into crystal form
        Dislocations (imperfections in lattice) make it easier to bend
        Impurities (imperfections in atom type) allow slippage of layers
        Work Hardening means hammer until impurities are together
        Heat: can soften by dispersing impurities or harden if control cooling
Notes: Mention shape memory alloys

## Slide 45: Defect Summary
Point, Line, Planar and Volumetric defects exist in solids.
The number and type of defects can be varied and controlled
  T controls vacancy concentration
  amount of plastic deformation controls # of dislocations
Defects affect material properties (e.g., grain boundaries control crystal slip, conductivity)
Defects may be desirable or undesirable
  e.g., dislocations may be good or bad, depending on whether plastic deformation is desirable or not.
Notes: Got to this slide in 50 minute lecture.